## Slide 1: Electronic Structure of Mn Ions in GaAs and (Ga,MnAs)
V.F. Sapega1,2
1
2

## Slide 2
Outline
Motivation
Introduction
Electronic structure of Mn acceptor in GaAs
  Raman study of Mn acceptor states in bulk GaAs
  Strain effect on Mn acceptor state in bulk GaAs
  Confinement effect on Mn acceptor state in GaAs:Mn/AlAs QW
States of Mn double donor in LT-GaAs
Conclusions

## Slide 3: Ferromagnetism in (Ga,Mn)As and its applications
H. Ohno et al., APL, 69, 363 (1996)
Magnetization vector manipulation
by electric fields
D. Chiba et al., Nature Lett. (2008)
Ferromagnetism in
(Ga,Mn)As DMS

## Slide 4: Models of the Mn acceptor in GaAs
i. hole enters the 3d5 shell, resulting in 3d4 configuration
magnetic susceptibility (1983)
Faraday-rotation (1985)
ii. 3d5 shell + weakly bound hole
Hot PL (1982)
EPR (1987)
Piezo-spectroscopy (1978, 1984)
Infrared Spectroscopy (1997)
Raman scattering (2000)
Mn 3d54s2
EA=113 meV
GaAs:MnGa

## Slide 5
I.Ya. Karlik, et al., Sov. Phys. Solid State, 1982
Antiferromagnetic exchange in 3d5 +h Mn acceptor
c(B) 0.5, B

## Slide 6
Mn acceptor electronic structure
2dh= 3 meV - K. Lassmann and Hp. Schad, Solid State Comm. 1976
2dh = 2.5 meV - Th.Frey et al, J.Phys.C: Solid State Phys. 1988
2dh = 9-12 meV - M. Linnarsson et al Phys. Rev. B 1997
g=2.77 – J.Schneider, et al., PRL 1987
N.S. Averkiev et al., Sov. Phys. Semicond. 1987
N.S. Averkiev et al., Sov. Phys. Solid State 1988
2dh = 10 meV
<1meV
g1*=7/4ge-3/4gh=2.74
g2*=11/12ge+1/12gh=1.94
c() =0.504

## Slide 7
Electronic Raman study of Mn acceptor state
V.F. Sapega, T. Ruf, M. Cardona, SSC 2000, and PSS(b) 2001.

## Slide 8: Spin flip Raman study of Mn acceptor state
V.F. Sapega, T. Ruf, M. Cardona, SSC 2000, and PSS(b) 2001.

## Slide 9
Strain effect on Mn acceptor state
N.S. Averkiev, et al, Soviet Phys. Semiconductors, 1987
P||[111]

## Slide 10
Strain effect on Mn acceptor state
P||[111]

## Slide 11
Strain effect on Mn acceptor polarization
B
P
Compressive strain applied perpendicular to magnetic field reduces
Mn acceptor polarization in a magnetic field.
V.F. Sapega, et al., SSC 2013
Notes: cheam

## Slide 12
The effect of confinement on Mn acceptor state
R1 MBE bulk GaAs:Mn
D1 MBE GaAs:Mn/AlAs (10/3)nm
D2 MBE GaAs:Mn/AlAs (12.5/3)nm
V.F. Sapega, et al., PRB 2007.

## Slide 13
The effect of QW confinement on Mn acceptor state
Random fields effect:
QW confinement effect:

## Slide 14
Mn acceptor states in GaMnAs DMS
LT-(Ga,Mn)As
x~5x10-5
V.F. Sapega, et al., PRB 2002
Single Mn acceptors exist even in heavily
doped (x<1-2%) (Ga,Mn)As DMS.

## Slide 15
Double Mn donor in LT GaAs:Mn

## Slide 16
Double Mn donor in LT GaAs:Mn

## Slide 17
Double Mn donor in LT GaAs:Mn

## Slide 18
Double Mn donor polarization in a magnetic field
Faraday geometry
T=4K
positively doubly charged Mn interstitials in GaAs act as double donors:
For He like atom:
Mn double donor:
N.S. Averkiev, A.V. Rodina, Sov. Phys. Solid State 1993

## Slide 19
Electronic structure of Mn acceptor in GaAs is studied by means of hot PL, electronic and spin-flip Raman scattering
The effect of confinement and uniaxial stress and magnetic field on Mn acceptor state is studied.
The exchange, deformationail energy and g factor of the Mn acceptor state are detemined
The states of Mn double donnor are observed in PL and their binding energies are measured.
Conclusions

## Slide 20
N.S. Averkiev, Ioffe Inst., SPb
M. Cardona, MPI, Stuttgart
T. Ruf, MPI, Stuttgart
K.H. Ploog, PDI, Berlin
I.V. Kraynov, Ioffe Inst., SPb
G.V. Dimitriev, Ioffe Inst., SPb
N.I. Sablinas, Ioffe Inst., SPb
I.E. Panaiotti, Ioffe Inst., SPb
Acknowledgements:

## Slide 21
Thank you for your attention

## Slide 22
Strain and magnetic field effect on Mn acceptor state
B
P